## Slide 1: “Development of a script-based package for analysis of work hardening behaviour”
Aman Sharma (17118013)
Supervised by – Dr Sumeet Mishra
Abhinav Garg (17118002)

## Slide 2: INTRODUCTION
Work hardening analysis of a material forms a foundation of further research in plasticity
Calculation of parameters like yield strength, Young’s modules etc. is a prerequisite before one can proceed with their main objectives
However, all these parameters were calculated semi-manually
Since these parameters were utterly important, we decided to automate this process

## Slide 3: OBJECTIVE
Create Jupyter notebook which automates the following:
Identify Young’s Modulus, Yield Strength, and Ultimate Tensile Strength.
Separate the plastic region
Return a work hardening plot
Fit different dislocation-density based model
Plot the YLD2000 yield criterion

## Slide 4: BASIC PREREQUISITES

## Slide 5: HOLLOMON EQUATION
1. It tends to predict infinite strength for materials being tested.
2. It does not provide information about the microstructure.
Parameter | Value
K | 812.9174 MPa
n | 0.15

## Slide 6: KOCKS-MECKING THEORY
The model is essentially a competition of two concurrent effects:
1. Accumulation of dislocation:
2. Dynamic recovery (annihilation):

## Slide 7: A TYPICAL KOCKS-MECKING PLOT

## Slide 8: IMPLEMENTATION OF THE KOCKS-MECKING MODEL

## Slide 9: COARSE GRAINED FOREST DISLOCATION DENSITY-BASED MODEL
Implementation of Kocks-Mecking Model for single phase and coarse-grained materials (T6 in our case).
Since,
(Voce equation)
Solving the equation

## Slide 10: GEOMETRIC OBSTACLE MODEL
Materials where spacing between dislocations is small.
Inaccurate fitting of Voce equation.

## Slide 11: HYBRID MODEL
This model combines the previous two models and gives the equation:
Inaccurate fitting of Voce equation

## Slide 12: ISOTROPIC YIELD CRITERION
TRESCA
VON MISES
The major drawback of these methods is that they can be applied to isotropic materials only
Notes: Tresca: Yield occurs when the maximum shear stress is equal to the shear stress at yielding in a uniaxial tensile test
Von mises: Yield occurs when the maximum distortion energy is equal to the distortion energy at yielding in a uniaxial tensile test

## Slide 13: BARLAT YLD2000 CRITERIA
Barlat proposed a series of models accounting for materials exhibiting planar anisotropy. Out of which the most popular was Yld2000-2d.

## Slide 14: COMPUTATION OF ANISOTROPIC PARAMETERS
3 stress states – RD, TD, and balanced biaxial
Index | Mode | 𝛾 | 𝛿 |  | 𝑝 | 
1 | Rolling () |  |  |  |  | 
2 | Transverse () |  |  |  |  | 
3 | Balanced biaxial |  |  |  |  | 
 | Mode | 𝛾 | 𝛿 |  | 𝑝 | 
1 |  |  |  |  |  | 
2 |  |  |  |  |  | 
3 | Balanced biaxial |  |  |  |  | 

## Slide 15
Barlat YLD2000 is a more generalised model as depicted below.
Tresca criteria
Von Mises criteria
All are equal and a = 1
All are equal and a = 2
YLD2000: A GENERAL CASE

## Slide 16: GRAPHICAL SIGNIFICANCE OF ANISTROPC PARAMETERS

## Slide 17: CONCLUSION
All of our implementations have been hosted on the GitHub repository.
The yield criterion which we calculated using the Barlat YLD2000 method can be further used in the future to draw Formability Limit Diagram which has great significance in the world of industrial metallurgy.

## Slide 18: THANK YOU